FRICTION TESTING: RESULTS AND ANALYSIS

Report Prepared by Adeline Sutphen

With thanks to Graeme Martin and Warwick Hill

for design and development of the testing device.

October 12, 2005

Purpose

To determine the coefficient of friction between a range of materials and door knob surfaces. A material with a high coefficient of friction is desired.

Delimitations

This study is not designed to test mechanical material properties such as abrasion resistance, durability, fatigue failure etc. These mechanical material properties and the coefficient of friction will be considered during the final material selection.

Tables of Materials/Samples

Table 1

Gripping Materials

Material					Durometer				Surface

40A Urethane				40A					Smooth

60a Urethane				60A					Smooth

Tan Rubber (natural)			40A-60A				Smooth

Yoga Mat (polyvinyl)			> 40A				Gridded Foam

Rugby Glove				?					Silicon Print (1mm)

Table 2

Gripping Surface – Door Knobs

Material						Radius (mm)			Mass (g)

Wooden						28.32					84.65

Porcelain						29.75					220.66

Brushed Aluminum				28.35					76.88

Brass							25.73					158.98

Table 3

Dimensions and Load of Testing Device

Component				Length (mm)		Weight (g)

Lever Arm				165.6				Negligible

Load Weight							Variable: 250 – 500

Diagrams of Testing Device

Figure 1

Front View of Torque Device

Door Knob

Load Weight

Grip Material

Grip Material

Lever Arm

Figure 2

Side View of Torque of Torque Device

l

Fpull

T1

T2

Figure 3

Front View of Torque Device

l

Fpull

T1

θ

Fpull

l

Graphs of Load Weight (g) vs. Coefficient of Friction

Graph 1

Brass Knob

Graph 2

Brushed Aluminum Knob

Graph 3

Porcelain Knob

Graph 4

Wooden Knob

Calculations

Assumptions: Fpull is read when the knob just begins to turn. This reading is thus as the curve boundary between static-kinetic coefficient on the graph below (Figure D).

Graph 4

Static-Kinetic Coefficient of Friction Graph

Source: www.ac.wwu.edu/~vawter/PhysicsNet/Topics/Dynamics/Forces/Normal.html

Figure 4

FBD Knob-Top Material Plate

Fn

Fu = m*g

Fapp

Ff

Torque Calculation

T1 = Fpull*l*cos(θ)	*neglect θ as it is very small at the time of slip

T2 = -T1

Normal Force Calculation

Fn  = Fu  = m*g

Application Force Calculation, Fapp

Fapp = T2 / radiusknob				Fapp = μs*Fn = μk*Fn = μ*Fn

Coefficient of Friction Calculation

μ = Fapp / Fn

Photos

Conclusion

Four different door knobs were tested with five different rubber and foam samples for their coefficient of friction. The above graphs show the coefficient of friction under various load weights for all door knobs and rubber and foam samples. As seen in the first friction study, the Tan Rubber consistently out-performed all other rubber and foam samples. The Tan Rubber is a natural rubber of unknown durometer and physical properties. It seemed softer than the 60A durometer urethane and harder than the 40A durometer urethane. The tan rubber seems more durable than some of the soft foams tested and is less tacky than the 40A urethane.

The polyvinyl yoga mat and the 40A urethane also performed very well. The polyvinyl yoga mat is soft foam that I suspect will rip and tear easily over time. The 40A urethane showed slightly lower coefficients of friction than the polyvinyl yoga mat, except in combination with the brushed aluminium door knob. The 40A urethane is not as fragile as the polyvinyl yoga mat, but is softer and tackier than the tan rubber.

The silicon printed rugby gloves and the 60A urethane performed poorly in comparison to the other three materials. Both of these materials allowed the knob to slip under very little torque.

The results of this study also show that higher durometer materials, such as the 60A urethane, are not desirable for gripping use in this project. Though the polyvinyl yoga mat material has a high coefficient of friction its other material properties may make it less desirable as a gripping material. Further study should be carried out with 30-50A durometer urethanes and natural rubbers.